Dryko™ Seal Aluminized Asphalt Roofing / Repair Membrane Installation Guide

| HTS Code: 6807.10.0000 | Version 1.0 ¦ BSKR Brands LLC | (321) 285-9908 |
| --- | --- | --- |

| ☀ | Temperature Range for Application |
| --- | --- |

Apply Dryko™ Seal only when ambient and surface temperatures are within the range below. Applying outside these limits reduces adhesion and may compromise the waterproof seal.

| Recommended Application Temp. | 40°F (4°C) to 120°F (49°C) |
| --- | --- |
| Service Temp. After Install | -40°F to 180°F (-40°C to 82°C) |
| Cold Weather Note | Store rolls at room temperature before use; cold rolls are stiff and harder to press flat |
| Hot Weather Note | In direct sun, shade the roll and work surface before application to prevent premature tack-off |

★  Never apply over frost, ice, or standing water. Check weather forecast — no rain for at least 24 hours after installation.

| 1 | Safety First |
| --- | --- |

- Work on a dry day with no rain in the forecast

- Wear gloves, safety glasses, and non-slip shoes

- Use a roof harness

- Keep out of reach of children

| 2 | Inspect and Prepare the Area |
| --- | --- |

- Remove loose shingles, debris, and damaged material

- Surface must be dry and structurally sound

| 3 | Clean the Surface |
| --- | --- |

- Brush off dust, granules, and moisture

- Wipe with a clean cloth if needed

- Let area fully dry before priming

| 4 | Apply Asphalt Primer (When Necessary) |
| --- | --- |

- Use a brush or roller

- Apply primer 2–4 inches beyond the hole on all sides

- Coat both exposed decking and surrounding shingles

- Allow primer to flash off until tacky (usually 10–20 minutes)

★  Primer ensures proper adhesion and long-term seal

| 5 | Cut the Membrane Patch |
| --- | --- |

- Cut aluminum-coated membrane large enough to overlap the hole

- Minimum overlap: 4–6 inches on all sides

- For larger holes, use a 36-inch wide roll for full coverage

| 6 | Apply the Aluminum-Coated Asphalt Membrane |
| --- | --- |

- Center the membrane over the hole

- Press down starting from the center outward

- Ensure aluminum side faces up

| 7 | Seal and Press |
| --- | --- |

- Firmly press membrane edges by hand or with a roller

- Remove air bubbles and wrinkles

- Make sure edges are fully bonded to shingles

| 8 | Final Inspection |
| --- | --- |

- Confirm full adhesion

- No exposed decking

- No lifted edges or gaps

★  Roof is now watertight, UV-protected, and sealed

BSKR Brands LLC • info@bskrbrands.com • www.bskrbrands.com