Dryko™ Seal Primer Water-Based Asphalt Emulsion Installation Guide

| HTS Code: 2715.00.0000 | Version 1.0 ¦ BSKR Brands LLC | www.bskrbrands.com |
| --- | --- | --- |

| ☀ | Temperature Range for Application |
| --- | --- |

Apply Dryko™ Seal Primer only when ambient and surface temperatures are within the range below. Applying outside these limits reduces adhesion and may compromise the waterproof seal.

| Recommended Application Temp. | 50°F (10°C) to 104°F (40°C) |
| --- | --- |
| Relative Humidity | Below 85% |
| Cold Weather Note | Do not apply below 50°F (10°C); product will not flash off properly and adhesion will be compromised |
| Hot Weather Note | Warmer temperatures accelerate drying; work efficiently to avoid premature tack-off |

★  Never apply over frost, ice, or standing water. Check weather forecast — no rain for at least 24 hours after installation.

| ⚠ | Safety First (Read Before Use) |
| --- | --- |

- Work on a dry day with no rain in the forecast

- Wear gloves, safety glasses, and non-slip shoes

- Use proper fall protection (roof harness) when working at height

- Avoid skin and eye contact

- Keep out of reach of children

- Use in a well-ventilated area

| 1 | Inspect the Area |
| --- | --- |

- Identify damaged or leaking section

- Ensure surface is structurally sound

- Fix major damage before applying primer

| 2 | Clean the Surface |
| --- | --- |

- Remove dirt, dust, loose granules, and old sealant

- Brush thoroughly

- Wipe with clean cloth if needed

- Surface must be completely dry

| 3 | Apply Primer |
| --- | --- |

- Use a brush or roller

- Apply an even coat

- Extend 2–4 inches beyond repair area

- Cover exposed decking and surrounding shingles

| 4 | Let It Set |
| --- | --- |

- Allow primer to flash off until tacky

- Do NOT apply membrane while primer is wet

| 5 | Ready for Membrane |
| --- | --- |

- Once tacky, apply aluminum membrane

- Adhesion will be significantly stronger

★  Primer ensures proper adhesion and long-term seal

| ★ | Pro Tips & Common Mistakes |
| --- | --- |

| Pro Tips - Apply only on dry surfaces - Do not over-apply - Warmer temperatures = faster drying - Use on concrete, metal, wood, and porous surfaces | Common Mistakes to Avoid - Applying on wet surfaces - Skipping surface cleaning - Applying membrane before primer is tacky - Using too much primer |
| --- | --- |

| ✓ | Performance Benefits |
| --- | --- |

| ⬆ Adhesion Strength | 🛡 Enhanced Waterproof Seal | ⏳ Extended Repair Life | ✔ Long-Term Durability |
| --- | --- | --- | --- |

| ↪ | Quick Summary |
| --- | --- |

| 1 CLEAN | 2 PRIME | 3 WAIT | 4 APPLY |
| --- | --- | --- | --- |

BSKR Brands LLC • info@bskrbrands.com • www.bskrbrands.com